## Course Overview / Description

## Course Title: Automotive Materials

Credit Points: 3

| Course Code | Campus | Career | School | Learning Mode | Teaching Period(s) |
| --- | --- | --- | --- | --- | --- |
| 0544962 | Davutpaşa Campus Faculty of Chemistry-Metallurgy Online | Undergraduate | Metallurgy and Materials Eng. | Face-to-Face | Oct. 05-2020, Jan. 2020 |

Course Coordinator			: Prof. Dr. Mustafa ÇİGDEM

Course Coordinator Phone		: +90 212 383 46 77

Course Coordinator Email		: cigdem@yildiz.edu.tr

Course Coordinator Location: KM-A 207

Pre-requisite Courses and Assumed Knowledge and Capabilities

Materials Science II, Industrial Materials, Heat Treatment, Plastic Deformation, Welding, Machining and Foundry Technology,

Course Description

The course aims to enable you to develop an understanding of materials requirements for the automotive industry with particular emphasis on the light-weighting, safety and energy absorption, recycling, whole life cost and globalization effects. Primary focus of the course is to provide a link between design, materials and manufacturing through a sound understanding of structure-processing-property relationship of automotive materials.

The course includes the following key topics:

- Introduction to automotive materials

- Automobile Components (Parts)

- Materials selection and databases

- Chassis

- Body

- Engine

- Advanced high strength steel:

- Aluminium alloys

- Magnesium and titanium alloys

- Engineering polymers: Property/processing relationship; temperature, time dependency of physical properties

- Composite materials

Objectives/Learning Outcomes/Capability Development

In summary this course develops the following student capabilities:

- Problem solving and decision making

- Advanced technical competence

- Working in teams and professional networks

- Professional, legal and ethical standards

Upon completion of this course, you will be able to

- select advanced materials for specific automobile components and applications

- make use of state-of-the-art materials selection database

- discuss and present your work within professional networks

- simulate and test advanced materials in order to determine their structure and property relationships

- select advanced materials for recycling and re-use while complying with the end of life legislations

- apply life cycle analysis to the selection of advanced materials

Overview of Learning Activities

Please refer to the hub.

Overview of Learning Resources

The electronic learning package

Lecture notes

Class materials

Recommended References

Other Resources as advised by the course coordinator.

Overview of Assessment

Assessment in this course is based on:

Mid-term exam, group project report and presentation and final exam results. Group project – Groups consisting of 3-4 students will each undertake a ‘materials and process selection’ project for an automotive component. The group will submit a technical report and present an oral summary of the work in ‘Microsoft Power-Point’ presentation format. 
The project will enhance your technical competency, and enable you to deliver innovative materials and process solutions which comply with material requirements of the automotive components. The materials selection methodology implemented in this project, will improve your problem solving, decision making, teamwork, and research skills. It is also a means through which you will achieve a holistic understanding of the product (automobile).

Laboratory experiment - A laboratory experiment involving materials testing will be conducted in the future. You will be required to submit laboratory reports.

Class activities - Students will have the opportunity to interact with each other and with the lecturer through class activities.

Final exam – Your understanding of the course material, and your ability to solve industry relevant problems, will be assessed through a written exam.