## Slide 1: Solidification of Multiphase Metals and Alloys (I)
.

## Slide 2
In the previous chapter the solidification of single-phase metals and alloys was considered with regard to both the constitutional and structural effects which occurred. In this chapter more complex alloys are treated in which two or more phases are present. Eutectics, peritectics and monotectics are considered first. Particles in melts and gases in melts are dealt with subsequently.

## Slide 3: Eutectics
In Greek words eu: easy, teksis: melting
Eutectic: Easy melting
Binary eutectics
Considering the alloy of eutectic composition, the component phases solidify simultaneously to give a structure consisting of an intimate mixture o these phases.
The different structures of eutectics are divided into three groups:
(i) rough-rough
(ii) rough-faceted
(iii) faceted-faceted
rough: α < 2 faceted: α > 2

## Slide 5
Most metallic eutectics fall into group (i) and during growth there is coupling between the phases. In coupled growth the two phases grow immediately adjacent to each other with solute movement between the liquid regions in front of each phase. The normal morphologies are lamellar or rod like. In the presence of impurities, cellular growth occurs and a structure of eutectic colonies result. In lamellar eutectics the interlamellar spacing, λ related to the growth rate R by
a relation predicted theoretically and confirmed experimentally.

## Slide 6
A lamellar eutectic (rough-rough)

## Slide 7
Lamellar eutectic in the lead-tin system

## Slide 8
Rod-like eutectic in the aluminium-Al3Ni system:
(i) transverse section, (ii) longitudinal section.

## Slide 9
Al-Al3Ni CE: 5.7 % Ni, 94.3 % Al

## Slide 10: Competitive Growth of Dendrites and Eutectics
In the solidification of a binary eutectic alloy, growth is regular, the solid/liquid interface is planar. However, when alloy composition departs from eutectic or when a third alloying element is present, the interface can become unstable for the same reason as in the case of a simple solid/liquid interface. As shown in figure two types of morphological instability can develop: single-phase and two-phase.

## Slide 11
Types of instability of a planar solid/liquid eutectic interface. (a) Single-phase instability leading to the appearance of dendrites of one phase. (b) Two phase instability leading to the appearance of eutectic cells or colonies in the presence of a third alloying element.

## Slide 12
(a) Schematic representation of the growth front of a lamellar eutectic growing with a curved cellular interface. Rods form at the cell boundaries. (b) Cross section through an impure lead-cadmium alloy showing the eutectic colony structure.

## Slide 14
For non-eutectic compositions (hypo or hyper eutectic) the eutectic reaction is preceded by primary-phase dendritic growth. The resulting structure consists of dendrites in a eutectic matrix.
Hypoeutectic alloy copper-silver system showing copper-rich dendrites in a matrix of eutectic colonies.

## Slide 16
With group (ii) eutectics the growth is still coupled with the faceted phase dominant. The resultant structure are less regular. The faceted phase is surrounded by the other phase except at the tips of the growing spikes. The important metallurgical systems of aluminium-silicon and iron-graphite are of this type. These two systems are both able to be structurally modified by the addition of small quantities of some elements.

## Slide 17
An irregular eutectic structure (rough-faceted)

## Slide 18
The normal eutectic structure in the aluminium silicon system

## Slide 20
Where both eutectic components are faceted (group (iii)) the growth is no longer coupled and the resulting structure is a random mixture of the two phases. This type of structure is uncommon in metallic systems, but is expected for non-metallic systems where the α-factors of components should be large.
Complex eutectic structure, both phases normally have faceted interfaces. No coupled growth. (faceted-faceted)

## Slide 21: Lamellar-rod transition
Another aspect of binary eutectic solidification which is of importance is the lamellar-rod transition. For alloys of eutectic composition the tendency is to form rods when one phase has a low volume fraction relative to the other and lamellar when the phase proportions are more nearly equal. It is generally accepted that this is controlled by interface energy considerations, although under some conditions the normal solidification variables (R and G at the solid-liquid interface) can influence morphology.

## Slide 22
The relative surface areas for lamellar eutectic arrangements, Sıı compared with those of fibers, So, or vice versa, as function of volume proportions: (a) is the volume fraction of the minor constituent; (b) is the volume fraction of the major constituent. Eutectic alloys having lamellar habit are marked X and those with a fibrous habit are marked O.

## Slide 23
The surface area associated with a fibrous system (So) is very sensitive to the volume proportions, rising from zero to a maximum value of 0.8, when the rods would tend to make contact. On the other hand, the surface area of lamellar array (Sıı) is independent of volume fraction since it is independent of lamellar thickness. If the interface energies were the same for lamellar and rods we would only expect the lamellar arrangement at volume fractions greater than about 0.3.
(Lamellar eutectic forms)

## Slide 24: Ternary eutectics
Complex lamellar
A triple lamellar ternary eutectic in the system cadmium (α)-tin (β)-lead (γ). The lamellar arrangment is αγβγαγ.

## Slide 25
Combined lamellar-rod-like
The complex ternary eutectic in the aluminium-copper-magnesium system. The lamellar phases are aluminium and CuAl2 and the fibrous phase is Mg-rich.

## Slide 26: Modification of eutectics
Structural modification is produced in the systems aluminium-silicon and iron carbon (graphite). Two points should be noted: (i) the modified structure has significantly improved mechanical properties, especially toughness, and (ii) the dendritic growth process is affected in such a way that primary dendritic growth occurs in what is nominally an alloy of eutectic composition.
Eutectic modificators for Al-Si alloys: Na or Sr (~0.01%)
Eutectic modificators for Iron-Carbon: Mg or Ce (~0.030%)

## Slide 27
The coarse silicon structure of slow-cooled alloys is altered if rapid growth rates are used. A similar effect is produced by adding modifier (Na or Sr) to the slow cooled alloys. The silicon morphology is basically the same in both the growth rate-modified and additive modified alloys.
The modification that occurs in the iron-carbon system is even more striking. In the normal structure of grey cast iron, graphite flakes in matrix is altered to graphite spheroids in matrix (ductile cast iron). In this case also there is a dramatic increase in mechanical properties, particularly toughness.
Modification effects growth process rather than nucleation.

## Slide 28
The normal (unmodified) eutectic structure in the aluminium silicon system.
Sodium modified aluminium-silicon eutectic alloy.
Na or Sr are surface active elements. The absorbed Na or Sr at the Si/liquid interface prevents the diffusion of Si to form the modified fine Si structure.

## Slide 29
SEM micrographs of aluminium-silicon alloys after heavy etching of the aluminium matrix: (a) coarse silicon structure of unmodified slow-cooled alloy; (b) filamentary silicon in a quenched alloy (growth rate modified); (c) filamentary silicon in sodium-modified alloy.

## Slide 30
(a) Normal as-cast grey cast iron showing flake graphites in pearlitic matrix. (b) Modified spheroidal graphite cast iron in pearlitic matrix. (Ductile cast iron)

## Slide 31: Nucleation of flake graphite
Oxide at the center can be oxides of Ba, Ca or Al.

## Slide 32: Nucleation of spheroidal graphite

## Slide 33: Growth of graphite in cast iron

## Slide 34
Mg addition for spheroidal graphite formation decrease levels of S and O by forming MgS and MgO compounds. These elements are surface active elements and reduce surface tension of molten iron. So in the presence of high S and O levels, graphite nucleus can change its shape and grow outside to austenite case. Thus lamellar graphite forms. With high surface tension condition in liquid iron, spheroidal nucleus can not change its shape and become a spheroidal graphite at he end of the solidification.

## Slide 35: Sphericity of graphite in ductile cast iron