## Slide 1: Growth
.

## Slide 2
After nucleation a first step is to consider the growing nucleus. This requires an examination of the nature of the interface between the growing solid and the liquid.
The structure and form of this interface influences both the microstructural morphology of the resultant solid and also the number and distribution of imperfections within the solid. It also has an effect on thermal and constitutional changes in the adjacent liquid and the interaction between these effects can in turn lead to growth modifications.
The rate of solidification (freezing) is usually controlled by the rate of heat removal. In most solid-state reactions growth is controlled by diffusion.
One of the main differences is that the latent heat of solidification is very much greater than the latent heat of solid state reactions.

## Slide 3: The structure of the interface
The interface can broadly be defined as the boundary layer between the liquid and the solid. It is normally described as «smooth» when the boundary is discrete and «rough» when the transition extends over a number of atomic layers. It was shown that starting with an atomically smooth surface and adding atoms at random the relative change in surface free energy
ΔFS : Change in surface free energy
N : Number of possible sites
k : Boltzmann’s constant
Tm : Equilibrium melting temperature
x : is the fraction of sites occupied

## Slide 4
α : A parameter determines structure of the interface during growth.
Lm : Latent heat of solidification
ξ : Crystallographic factor
Crystallographic factor is a fraction of binding energy or coordination number of atoms one at the surface other at the inside of the crystal. It is always lower than unity (one) and has maximum value at close packed planes. It is equal of higher than 0.5 in these planes.

## Slide 6
Relative change in surface free energy as a function of the fraction of surface sites which are occupied. α depends on the crystal face, the type of crystal and the phase from which the crystal is growing.
* In some sources instead of α, term can be used

## Slide 7
α = 0.5

## Slide 8
α = 1

## Slide 9
α = 3

## Slide 10
α = 5

## Slide 11
α = 8

## Slide 12
α = 10

## Slide 13
Two distinct types of interface can be deduced from these figures.
1. α ≤ 2 : The interface has a minimum energy when approximately half of the sites are occupied.
«Rough Surface»
2. α ≥ 5 : The relative free energy is at a minimum when there are only a few occupied sites or a few unoccupied sites.
«Smooth or faceted surface»

## Slide 14
Most metals have α ≤ 2
Inorganic or organic liquids normally have α ≥ 5
A small group of materials e.g. silicon, bismuth which occupied middle group α = 2 - 5
They show complex or mixed growth.

## Slide 15: Growth of the interface
The growth rate of a crystal depends on the difference between the rate at which atoms add themselves to the interface and the rate at which they leave the interface. The normal procedure is to define a mechanism and calculate the mean rate of interface motion as a function of the undercooling ΔT.
The normal growth mechanism
Growth by repeated surface nucleation
Growth by imperfections

## Slide 16
Normal growth
In normal growth, all sites on the interface are considered to be equivalent and the interface advanced by the continuous random addition of atom.
R: mean growth rate, µ1: constant
For normal growth the growth rates can be quite high and the requirement of site equivalence implies the need for a rough interface. This is the growth mechanism considered applicable to most metals.
Since the materials with rough interfaces also tend to have low latent heats of melting, the rapid growth rates are comparatively easily sustained.

## Slide 17
Growth by surface nucleation
This theory assumes that the crystal interface is smooth (faceted) and that growth proceeds by the homogeneous nucleation of new layer in the form of disc nuclei which growth laterally until a complete layer is formed
µ2 and b are constants

## Slide 18
Schematic view of the formation of disc-shaped nuclei on a crystal. (a) view parallel to the surface; and (b) view normal to the surface.

## Slide 19
Growth on imperfections
Here the assumption is that some form of continuous growth step exists at which atoms can be added. The simplest form of the step is that formed when a screw dislocation emerges at a crystallographically smooth interface.
In this case the predicted growth rates are also very low and this a consequence of the restriction on the number of available growth sites.
Nevertheless the faceted growth of non-metals has been observed to involve this mechanism. Spiral growth on screw locations is common during the growth of crystal form solutions or from the vapour.

## Slide 20
Schematic view of a crystal containing a screw dislocation running normal to the upper surface. This surface is a spiral ramp and cannot be eliminated by adding atoms as shown.

## Slide 21
A growth spiral on a crystal SiC grown from the vapour

## Slide 22: Growth defects
Atomic scale defects e.g. vacancies, dislocations can be produced during crystal growth.
The equilibrium concentration in the solid decreases exponentially as the temperature decreases and rapid cooling of the solid can lead to supersaturation.
In the presence of impurities when cellular or dendritic interfaces are formed a well developed dislocation substructure is produced
The presence of impurity particles also leads to the development of the dislocation array of sub-boundaries produced during solidification, known as the lineage structure.