## Slide 1: SOLIDIFICATION PRINCIPLES

## Slide 2: Course Content / Subject Headings
Liquid metals
Nucleation
- Homogeneous and Heterogeneous
- Dynamic nucleation
Growth
- The structure of the interface (in atomic scale)
Solidification of Single Phase Metals and Alloys
- Pure metals
- Solute redistribution effects in alloys
- Constitutional undercooling (super cooling) in alloys
- Cellular and dendritic structures
- Dendrite arm spacing (DAS)

## Slide 3
Solidification of Multiphase Metals and Alloys
- Eutectics. Modification of eutectics (Cast iron and Al-Si alloys)
- Pretectics, Monotectics
Particles and Inclusions in Melts
Gasses in Melts
- Bifilm theory
The structure of Castings (Ingots)
- Macrostructure of fusion welds
Segregation
- Micro and Macro segregation
- Segregation patterns in ingots
Semi-Solid Metal Processing

## Slide 4: Liquid Metals
The principal approaches to the study of liquids came from two directions. Liquids were considered as either dense gases or rather disordered solids. Also a geometrical concept in which the liquid is considered as a heap of atoms or molecules has been the subject of study.

## Slide 5
Experimental Considerations
The change in volume on melting

## Slide 6
For close-packed metals, (hcp and fcc), melting causes a volume increase of 3.5-6 %. For most bcc metals the volume increase is 1-3%. Elements for which packing in the solids not dense (Si, Ge, Bi, Ga etc.) actually expand when they solidify.

## Slide 7
The latent heat of melting (fusion)

## Slide 8
The entropy of melting

## Slide 9
Diffraction studies of liquid structure

## Slide 12
Atomic spacing refers to the distance between the nuclei of atoms in a material.
According to diffraction studies:
The average interatomic separation in the liquid is slightly greater than in the solid.
The coordination number in the liquid is less than in the solid and usually in the range 8-11.

## Slide 13
These experimental considerations show that there is a relatively large increase in entropy on melting, particularly when the small change in coordination is taken into account This indicates that here is a considerable loss of order on melting without a large change in the separation of individual atoms or of the number of the neighbour atoms.

## Slide 14: Theories of liquid structure
Theories of liquid structure can be divided into those which consider the liquid as a dense gas (condensation theories) those which consider the liquid as disordered solid (lattice theories) and the geometrical theories)

## Slide 15
Lattice theories
These theories all use as a starting point a crystal lattice.
The cell theory in which melting is considered as a type of order-disorder reaction in which atom continue to be confined to the vicinity of a lattice site but are allowed to oscillate randomly and independently.
The hole or free volume theory which treated the liquid as a pseudo lattice which a large number of vacant sites.
The significant structures theory in which the liquid state involves partition between crystal like and gas like components

## Slide 16
Geometrical theories
The basic concept in this case is of a liquid as a heap of atoms or molecules.