## Slide 1
.
Solidification of Single Phase Metals and Alloys (II)

## Slide 2: Complete mixing in the liquid
If conditions of complete mixing by convection or stirring exist within the liquid, then with k0 < 1 the solute rejected at the interface is distributed evenly throughout the liquid. Thus in the initial stages, where the volume of liquid is large, the overall change in composition is small. As solidification proceeds, however the compositional changes in the liquid become more marked.

## Slide 3
Concentration-distance profiles for a bar solidified under conditions of complete solute mixing in the liquid

## Slide 4: Partial mixing in the liquid
The effect of the mixing conditions on the nature of the solute layer at the interface: (a) no mixing diffusion only; (b) partial mixing; (c) complete mixing

## Slide 5
The intermediate case in which partial mixing in the liquid is produced by the combined effect of diffusion and convection or stirring was examined. In the analysis the thickness of the diffusion boundary layer (δ) decreased with increased mixing varying from about 10-2 mm for vigorous stirring to about 1 mm for natural convective stirring.
x (distance)= fs

## Slide 6
Solute distribution in a solid bar frozen from liquid of initial concentration C0, for: (a) equilibrium freezing; (b) solute mixing in the liquid by diffusion only; (c) complete solute mixing in the liquid; (d) partial solute mixing in the liquid.

## Slide 7: The effect of growth rate changes
If we consider solute profiles of this figure, we can see that the total amount of solute incorporated into the diffusion boundary layer increases as the growth rate decreases and vice versa. Thus if a fluctuation in the growth rate occurs during solidification of an alloy with k0 < 1, the amount of solute in the interface pile-up will need to increase if the growth rate slows down or to decrease if the growth rate speeds up. These changes will lead to a localised deviation from the steady state while the solute pile-up changes.

## Slide 8
The need for an increase in the amount of solute in the pile-up with a decreased growth rate means a local decrease in the amount of solute deposited in the solid as the growth rate changes. Thus a region depleted in solute will appear in the solid. The reverse is true if the growth rate is increased. The result in the two cases is shown in this figure. Only with complete mixing in the liquid is no solute banding to be expected as the growth rate fluctuates.
The effect of changes in the growth rate on the localised solute distribution in the solid: (a) growth rate decreased; (b) growth rate increased.

## Slide 9: Constitutional Undercooling (Supercooling) in Alloys
Tİ= interface temperature
TA = actual temperature in the liquid

## Slide 11
Constitutional undercooling ahead of an interface showing two applied temperature gradients.
Such a condition is called constitutional undercooling because it results from compositional (constitutional) variations)

## Slide 12
The magnitude of the undercooling ahead of an interface when constitutional supercooling exist.

## Slide 13
For no constitutional undercooling we require that:
G and R are process parameters
m, C0, D and k0 are material and system parameters

## Slide 14
The nature of this equation allows us to define conditions which will favour constitutional undercooling. These are:
Low temperature gradients in the liquid.
Fast growth rates.
Steep liquid lines.
High alloy contents (constitutional undercooling normally exist for C0 ≥ 0.2 %)
Low diffusivity in the liquid.
Very low k0 for k0 < 1 or very high k0 for k0 > 1.

## Slide 15
In the presence of constitutional supercooling the undercooling is,
The maximum undercooling occurs at a point given by

## Slide 18
In cellular growth, the primary arms extend into the liquid but there are no secondary dendrite arms.
In independent growth nucleation occurs in front of the interface