## Slide 1: Solidification of Single Phase Metals and Alloys (I)
.

## Slide 2
In this chapter we will be concerned with the effect of the different solidification variables (e.g. growth rate and temperature gradient in the liquid) on the structure and composition of the growing solid. In particular, when we consider single-phase alloys, the way in which the solute redistributed during solidification will be examined as will the effects of this redistribution on the micro and macro structure of the solidifying alloy. Before examining the solidification process it is essential to define clearly a terminology.

## Slide 3: Terminology
Growth Rate (R): is a measure of the rate of advance of the interface between the liquid and the solid.

## Slide 4
Temperature Gradient (G) (in the liquid) is usually taken to refer to the gradient in the liquid away from the interface in the direction of growth. If the temperature increases as we go into the liquid, the temperature gradient is considered to be positive and vice versa. Commonly, temperature gradients vary from a few degrees centigrade per centimetre during the growth of single crystals, to tens of degrees centigrade per centimetre in castings and ingots, and to hundreds of degrees centigrade per centimetre during weld-pool solidification.

## Slide 6
Diffusivity (Diffusion Coefficient, D):
Determines the rate at which atoms can move in the liquid. For virtually all metallic liquids D is of the order of 5 x 10-5 cm2/sec. Diffusion rates in the solid are much smaller ~10-8 cm2/sec. for common metals just below their melting points. Thus solute redistribution in the solid is usually ignored in comparison to solute redistribution in the liquid.

## Slide 7
The equilibrium distribution coefficient, k0
İs defined by the phase diagram, assuming the liquidus and solidus lines to be straight. The equilibrium distribution coefficient is given by the ratio:

## Slide 10
If the effect of the solute is to lover the liquidus temperature then k0 < 1 and vice versa.
It is sometimes convenient to define an effective distribution, kE as
Scheil Equation
fs: fraction solidified

## Slide 11
Slope of the liquidus line (m)
Positive (m) Negative (m)
Although this is contrary to normal mathematical practice, this convention has been adhered to throughout the literature on solidification.

## Slide 12
Unidirectional Solidification
(a) A casting boat (graphite) used for controlled directional solidification (schematic). The metal is shown as partially solidified. (b) Schematic view of the cross section of a partially solidified ingot showing how the casting boat can be considered as a section of the ingot.

## Slide 13
Cooling curves
(a) Cooling curve for a pure metal that has not been well-inoculated. The liquid cools as specific heat is removed (between points A and B). Undercooling is thus necessary (between points B and C). As the nucleation begins (point C), latent heat of fusion is released causing an increase in the temperature of the liquid. This process is known as recalescence (point C to point D). The metal continues to solidify at a constant temperature (Tmelting). At point E, solidification is complete. The solid casting continues to cool from this point. (b) Cooling curve for a well-inoculated, but otherwise pure, metal. No undercooling is needed. Recalescence is not observed. Solidification begins at the melting temperature.

## Slide 14: Pure metals: Interface forms
(a) Area of solid and liquid adjacent to the interface showing positive temperature gradients in the liquid and solid (schematic). Gsolid is steeper than Gliquid because of the higher thermal conductivity of the solid. (b) Schematic sequence showing the formation of an unstable protuberance which melts because the local tip temperature exceeds the melting temperature.

## Slide 15
(a) Area of solid and liquid adjacent to the interface showing a negative temperature gradient in the liquid and a positive temperature gradient in the solid (schematic.) (b) Schematic sequence showing the formation and stabilisation of a protuberance on the interface when it projects into a region where the local tip temperature is below the melting temperature.

## Slide 16
When the temperature of the liquid is above the freezing temperature, a protuberance on the solid-liquid interface will not grow, leading to maintenance of a planar interface. Latent heat is removed from the interface through the solid.

## Slide 17
Planar Growth: When a well-inoculated liquid (i.e., a liquid containing nucleating agents) cools under equilibrium conditions, there is no need for undercooling since heterogeneous nucleation can occur. Therefore, the temperature of the liquid ahead of the solidification front (i.e., solid-liquid interface) is greater than the freezing temperature. The temperature of the solid is at or below the freezing temperature. During solidification, the latent heat of fusion is removed by conduction from the solid liquid interface. Any small protuberance that begins to grow on the interface is surrounded by liquid above the freezing temperature The growth of the protuberance then stops until the remainder of the interface catches up. This growth mechanism, known as planar growth, occurs by the movement of a smooth solid-liquid interface into the liquid.

## Slide 18
(a) If the liquid is undercooled, a protuberance on the solid-liquid interface can grow rapidly as a dendrite. The latent heat of fusion is removed by raising the temperature of the liquid back to the freezing temperature. (b) Scanning electron micrograph of dendrites in steel (x15).

## Slide 19
Dendritic Growth: When the liquid is not inoculated and the nucleation is poor, the liquid has to be undercooled before the solid forms. Under these conditions, a small solid protuberance called a dendrite, which forms at the interface, is encouraged to grow since the liquid ahead of the solidification front is undercooled. The word dendrite comes from the Greek word dendron that means tree. As the solid dendrite grows, the latent heat of fusion is conducted into the undercooled liquid, raising the temperature of the liquid toward the freezing temperature. Secondary and tertiary dendrite arms can also form on the primary stalks to speed the evolution of the latent heat. Dendritic growth continues until the undercooled liquid warms to the freezing temperature. Any remaining liquid then solidifies by planar growth.

## Slide 20
The difference between planar and dendritic growth arises because of the different sinks for the latent heat of fusion. The container or mold must absorb the heat in planar growth, but the undercooled liquid absorbs the heat in dendritic growth. In pure metals, dendritic growth normally represents only a small fraction of the total growth and is given by
where c is the specific heat of the liquid. The numerator represents the heat that the undercooled liquid can absorb, and the latent heat in the denominator represents the total heat that must be given up during solidification. As the undercooling ΔT increases, more dendritic growth occurs. If the liquid is well-inoculated, undercooling is almost zero and growth would be mainly via the planar front solidification mechanism.

## Slide 21
Typical form of cooling curve for pure metals showing the regions in which the different growth phenomena occur.

## Slide 22: Solute Redistribution Effects in Alloys
The growth of impure metals is much more complex because of the redistribution of solute that occurs during solidification. This can produce changes in the growth morphology and lead to solute segregation on both a microscale and a macroscale. If we consider the initial sequence of events during the solidification of an alloy of composition C0, with distribution coefficient k0 < 1, it is clear from the phase diagram that the first solid to form will have composition of C0k0. Since k0 < 1 is a small localised increase in the solute content of the liquid. First, the solute increase may disperse in the liquid by diffusion only. Alternatively, conditions of complete mixing in the liquid which rapidly spread the excess solute throughout the bulk of the liquid.
For solute concentrations (C0) higher than about 0.5 % the solute pile-up effects are very marked and the physical nature of the interface alters to a non-planar configuration.

## Slide 23: Solute redistribution by diffusion
Portion of a phase diagram for an alloy of composition C0, with k0 < 1 showing initial compositional changes.
The solute profile ahead of the interface during steady-state solidification with solute redistribution by diffusion only (k0 < 1)

## Slide 26
Concentration-distance profiles for a bar solidified under condition where solute transport in the liquid is by diffusion only. (a) k0 < 1; (b) k0 > 1.