## Slide 1: Solidification of Multiphase Metals and Alloys (II)
.

## Slide 2: Peritectics
In Greek words, Peri: around or surrounding
Teksis: melting
Peritectic reaction:
L + α  β
or
L + S1  S2

## Slide 4
When the primary phase has cooled to the peritectic temperature (Tp) it should react with the liquid to form second component phase. In practice it becames quickly encapsulated by the second phase and the reaction is stifled by the need for diffusion through this solid layer.
The peritectic reaction should seldom proceed to completion.

## Slide 7
This diagram shows that, under equilibrium conditions, all alloys to the left of I will solidify to α crystals. Similarly, all alloys to the right of III will solidify to β crystals. Alloys between II and III first solidify to α crystals and then transform to stable β crystals. Alloys between I and II also solidify to α crystals, but they are partially transformed to β crystals later. The volume fraction of each phase is determined with the lever rule if the alloy solidifies under equilibrium conditions. In practice, the lever rule usually will not give the volume fraction of the different phases, because the nucleation and growth kinetics, determined by the diffusion rate, in the solid phases determine the time required to reach equilibrium.

## Slide 8: Mechanisms of Peritectic Formation
Peritectic reactions or transformations are very common in the solidification of metals. Many interesting alloys undergo these types of reactions—for example, iron-carbon and iron-nickel-base alloys as well as copper-tin and copper-zinc alloys. The formation of peritectic structures can occur by at least three mechanisms:
Peritectic reaction, where all three phases (α, β, and liquid) are in contact with each other
Peritectic transformation, where the liquid and the α solid-solution phase are isolated by the β phase. The transformation takes place by long-range diffusion through the secondary β phase.
Direct precipitation of β from the melt, when there is enough undercooling below the peritectic temperature, Tp. Direct precipitation of β from the melt can occur when a peritectic reaction or peritectic transformation is sluggish, as is often the case.

## Slide 9
Peritectic reactions can proceed only as long as α and liquid are in contact. The β-phase solid nucleates at the α-liquid interface and readily forms a layer isolating α from the liquid. This mechanism occurs from short-range diffusion. In contrast, the term peritectic transformation is used to describe a mechanism of long-range diffusion, where A atoms and B atoms migrate through the α layer to then form the β-phase solid at the α-β and the β-liquid interfaces, respectively.
From the final microstructure, it is not apparent by which mechanism β has formed. In any case, all three of the mechanisms require some undercooling, because the driving force is zero at the peritectic temperature. The time dependence is pronounced for the peritectic transformation. Therefore, the amount of β phase formed will depend on the cooling rate or on holding time if isothermal conditions are established.

## Slide 10
Mechanisms of peritectic reaction and transformation. (a) Lateral growth of a β layer along the α-liquid interface during peritectic reaction by liquid diffusion. (b) Thickening of a β layer by solid-state diffusion during peritectic transformation. The solid arrows indicate growth direction of β; dashed arrows show the diffusion direction of the atomic species.

## Slide 11
Primary UAl3 (gray) partially surrounded by peritectically-formed UAl4 (dark) in an Al-6U alloy that was cooled slowly from above liquidus to 760 °C (1400 °F) and held 10 min, then cooled to 670 °C (1240 °F) and held 15 min (peritectic temperature: 732 °C, or 1350 °F). The matrix is aluminum (white) with UAl4 (dark) eutectic. This UAl3 + Al  UAl4 reaction leads to unfavorable rolling behavior. Original magnification: 700x.

## Slide 13
Start of the peritectic transformation directionally-solidified Cu-20Sn. Note the homogeneous thickness of the β layers (gray) around the primary α (white). The matrix (dark) is a mixture of tin-rich phases. Original magnification: 160x

## Slide 15
Peritectic transformation of an Sb-14Ni alloy that was slowly cooled to 650 °C (1200 °F) and held 1 h, then cooled to 615 °C (1140 °F) and held 10 min (peritectic temperature: 626 °C, or 1159 °F). An irregular layer of NiSb2 crystals (dark) is formed around the coarse primary NiSb crystals. The matrix is the coarsened NiSb2-Sb eutectic. Original magnification: 200x.

## Slide 17
Peritectic Cascades. In many systems, one peritectic reaction at a high temperature is followed by one or more peritectic reactions at lower temperatures. If the diffusion rate is low in the initially formed peritectic layer, a second peritectic layer can be formed when the second peritectic temperature is reached. This type of series of peritectic reactions is referred to as a cascade. The individual thicknesses depend on the growth rate and the rate of consumption by other growing phases, that is, on the diffusivities and the molar volumes of the individual phases.
For example, the binary tin-antimony systems exhibit a peritectic cascade. In this case, it is possible to get layers of each phase around the initial pro-peritectic phase. The cascade in the phase diagram for this alloy includes a peritectic and a peritectoid transformation.

## Slide 18
Microstructure of a Sn-50wt%Sb alloy. The primary β phase is light, surrounded by a dark gray structure that was originally Sb2Sn3 but has decomposed to β + Sn. Original magnification: 50x.

## Slide 20: Monotectics
Monotectic reaction: a liquid phase transforms into a solid phase and another liquid phase.
L1  α + L2

## Slide 23
The solidification of alloys with a liquid miscibility gap, called monotectic alloys, is puzzling since decades especially compared to eutectic solidification to which they seem very similar. Alloys with exact monotectic composition solidify at the monotectic temperature by decomposition into a solid and a liquid phase and thus differ from eutectic ones only by the occurrence of a liquid phase at the nonvariant point. Alloys with hypermonotectic composition have to pass the liquid miscibility gap and thus a large region ahead of the monotectic reaction front is thermodynamically in a two-phase liquid state.
Four different microstructures are observed in solidification of such alloys: fibrous arrangement of the liquid phase, string of pearls, irregularly dispersed droplet and fully segregated two layer arrangement.

## Slide 24
Alloys with a liquid miscibility gap are quite common Binary alloys like Cu-Pb, Al-Pb, Al-In, Al-Bi, Fe-Ag, Ag-Ni are a few examples. The immiscibility typically is observed if the alloy components have a huge melting temperature difference and a positive enthalpy of mixing. The critical temperature of this gap is typically far above the melting point of the higher melting component. For an alloy whose gross composition is inside the miscibility gap two liquid phases are in equilibrium for temperatures above the monotectic one. These two liquids typically have a huge density difference leading to a very rapid sedimentation and macro-segregation. At the monotectic point three phases coexist and the monotectic reaction takes place: the L1 liquid decomposes into a solid of almost pure A and an L2 liquid rich in B. With the exception of Cu-Pb and Al-In the monotectic point (Tmono, Cmono) is always close to the component with the higher melting point.

## Slide 25
Transverse section of transition regions showing composite and dendritic structures: copper – light phase, lead – dark phase.

## Slide 26
Microstructures of the specimens of (a) Fe–Sn and (b) Cu–Pb alloys. The corresponding compositions are marked as dashed lines in the phase diagrams. The critical compositions of the two alloys are Fe–68 wt%Sn and Cu–64 wt%Pb, respectively. The dark phase is L2, Sn-rich or Pb-rich low melting temperature phase, while the light one is L1, Fe-rich or Cu-rich high melting temperature phase.

## Slide 27: Particles and Inclusions in Melts
Foreign particles which do not dissolve in either the liquid or the solid are often present during solidification.
Insoluble Particles
Exogeneous
Come from external sources (Mould, ladle, dross, ladle).
Endogeneous
Arise from reactions within the solidifying metal.

## Slide 28
For each system it was found that there was a critical growth rate below which the particles were pushed by the interface and above they were trapped in solid.

## Slide 29
Towards the end of a solidification process, however as the growth rates slow down, it is possible for particles to be swept together to produce quite deleterious accumulations inclusions.
In some cases the particles appear to have become grown-in because they have been trapped in isolated regions of liquid by the growth of dendrite branches.
Generally the critical growth rates were all low (~10-3 cm/sec). It is thus expected that entrapment will occur in most practical cases.
It is also possible for the solid inclusions to act as sites for heterogeneous nucleation and it is recognised that they have an important role in ingot solidification.
The constraints imposed on particle movement by the existence of a solid network in the liquid make predictions of particle distributions very difficult.

## Slide 32
Pile-up of particles at a solid-liquid interface at low growth rate in the system thymol-zinc

## Slide 33
Entrapped inclusions and precipitates in Al-Si-Cu-Mg alloy

## Slide 34: Gases in Melts
Apart from the possibility of gases being trapped inadvertently during casting, considerable difficulties can result from the marked differences in the solubility of gases in liquid and solid metals.
Solubility of hydrogen in aluminium

## Slide 35
Under these conditions it is expected that the gas will come out of solution and appear as bubbles of one form or another.
It is recognised that the nucleation of gas bubbles should be difficult, but shrinkage may make an important contribution to pore nucleation, as may the presence of certain inclusions.
In all cases, because of he local supersaturation the solid-liquid interface should be preferred site after nucleation the bubble can behave in a number of different ways.
2Al + 3H2O  Al2O3 + 6H
Moisture Oxide Solute
in air formation hydrogen

## Slide 36
It can float away, collecting gas in the process, and escape from the liquid at a free surface.
It can move with the interface, growing at the same time to become entrapped in due course.
It can become incorporated into the interface to grow as an elongated blowhole.
It can be rapidly overgrown by the interface and become entrapped.
With long dendrites, the gas bubbles are trapped and the result is gas porosity. With short dendrites, elongated tubes of gas (worms) may form. (Gas worms in ice cubes)

## Slide 38
The amount of gas that can be dissolved in molten metal is given by Sievert’s Law:
Pgas: Partial pressure of the gas in contact with the metal
K is a constant which for a particular metal-gas system, increases with increasing temperature.
PA: Atmosphere pressure
PM: Metallostatic pressure
Pγ Surface tension pressure
Pγ = 2γ/r
Homogeneous nucleation of hydrogen gas bubbles is very difficult. Partial pressure must be ~30.000 atm.

## Slide 39
When gasses dissolve in liquid metals, they usually dissolve monoatomically.
H2 2H, N2  2N, O2 2O
In addition to monoatomic gases, carbon monoxide and water vapour are soluble in metals.
CO  C + O and H2O  2H + O
Hydrogen is soluble in almost all liquid metals, but the solubility of nitrogen and carbon is limited in non-transition metals.

## Slide 40: Double Oxide Film (Bifilm) Theory

## Slide 41
Surface oxide film of aluminium melt is not harmful as long as it remains on top of the surface. The problem with an oxide film only occurs when it becomes a submerged film. When the molten aluminium containing the surface oxide film is poured into the mould, the surface oxide film may be folded over or broken by the action of a breaking wave or by droplets forming and falling back into the melt which results in entrainment of the surface film in the bulk liquid. These folded films will trap gas between the dry interfaces and the outer side and are strongly bonded (surface oxide have grown atom-by-atom from the melt) with the matrix when metals solidify. These folded oxide films in the casting are known as double oxide films or bifilms.

## Slide 43: Reduced Pressure Test (RPT)
RPT is an inexpensive and effective way to determine hydrogen levels in aluminum, and used by thousands of aluminum foundries to control gas porosity.
A small sample of the molten aluminum is taken from the melt and immediately placed under a vacuum dome of a Reduced Pressure Tester. The sample is allowed to solidify for approximately 7 minutes at 25 to 28 inches-Hg vacuum. Solidifying under vacuum expands the volume of hydrogen gas approximately 10X greater than solidification at normal atmosphere. This expansion of hydrogen porosity in the sample makes it possible to measure and evaluate various gas levels in the melt.
Evaluation techniques
Visual comparison to gas chart
Specific gravity (density)