## Slide 1: Cast Irons .

## Slide 2
Cast irons are kinds of iron alloys which include carbon up to 4 % and silicon up to 3.5 %.
Historically, the first classification of cast iron was based on its fracture. Two types of iron were initially recognized:
White iron: Exhibits a white, crystalline fracture surface because fracture occurs along the iron carbide plates; it is the result of metastable solidification (Fe3C eutectic)
Gray iron: Exhibits a gray fracture surface because fracture occurs along the graphite plates (flakes); it is the result of stable solidification (Gr eutectic).

## Slide 3
With the advent of metallography, and as the body of knowledge pertinent to cast iron increased, other classifications based on microstructural features became possible:
Graphite shape: Lamellar (flake) graphite (FG), spheroidal (nodular) graphite (SG), compacted (vermicular) graphite (CG), and temper graphite (TG); temper graphite results from a solid-state reaction (malleabilization)
Matrix: Ferritic, pearlitic, austenitic, martensitic, bainitic (austempered)
This classification is seldom used by the floor foundryman. The most widely used terminology is the commercial one. A first division can be made in two categories:
Common cast irons: For general-purpose applications, they are unalloyed or low alloy
Special cast irons: For special applications, generally high alloy

## Slide 4
Classification of cast irons

## Slide 5
Classification of special high-alloy cast irons.

## Slide 7
Gray Cast Iron – DIN EN 1561 |  | 
Grade | Material No. | DIN 1691
EN-GJL-150 | EN-JL 1020 | GG-15
EN-GJL-200 | EN-JL 1030 | GG-20
EN-GJL-250 | EN-JL 1040 | GG-25
EN-GJL-300 | EN-JL 1050 | GG-30
EN-GJL-350 | EN-JL 1060 | GG-3
Spheroidal Graphite Cast Iron – DIN EN 1563 |  | 
Grade | Material No. | DIN 1693
EN-GJS-350-22 | EN-JS 1010 | GGG-35.3
EN-GJS-400-18 | EN-JS 1020 | GGG-40.3
EN-GJS-400-15 | EN-JS 1030 | GGG-40
EN-GJS-450-10 | EN-JS 1040 | GGG-40
EN-GJS-500-7 | EN-JS 1050 | GGG-50
EN-GJS-600-3 | EN-JS 1060 | GGG-60
EN-GJS-700-2 | EN-JS 1070 | GGG-70
EN-GJS-800-2 | EN-JS 1080 | GGG-80

## Slide 8
Iron-carbon phase diagram at 2.5% Si.

## Slide 9
Both carbon and silicon influence the nature of iron castings. It is therefore necessary to develop an approximation of their impact on solidification. This has been accomplished through development of the concept of carbon equivalence (CE). Using this approach, carbon equivalence is calculated as:
CE = %C + %Si/3 (Eq 1)
or more precisely, taking phosphorus into consideration:
CE = %C + (%Si + %P)/3 (Eq 2)
Using Eq 1 and 2, it is possible to relate the effect of carbon, silicon, and phosphorus to the binary iron-carbon system. Irons with a carbon equivalent of 4.3 are considered to be of eutectic composition. Most gray irons are hypoeutectic (that is, CE < 4.3). Nearly all of the mechanical and physical properties of gray iron are closely related to CE value.

## Slide 10
Simplified iron-carbon-silicon phase diagram at 2% Si.

## Slide 11
At temperatures above point 1 in figure above, the iron is entirely molten. As the temperature is decreased and the liquidus line is crossed, primary freezing begins with the formation of proeutectic austenite dendrites. These dendrites grow and new dendrites form as the temperature drops through the primary freezing range, which is marked by points 1 and 2. Dendrite size is governed by the carbon equivalent of the iron and the solidification rate. Lower carbon equivalents produce large dendrites because the temperature interval between the liquidus and eutectic lines is greater for these irons than for those with a higher carbon equivalent. As expected, rapid cooling promotes a finer dendrite size.

## Slide 12
During the formation of the austenite dendrites, carbon is rejected into the remaining liquid. The carbon content of the liquid increases until it reaches the eutectic composition of 4.3%. Once this composition is attained, the liquid transforms into two solids. This takes place between points 2 and 3. The type of solid formed depends on whether solidification is following the metastable or stable eutectic reaction. Iron carbide plus austenite form during the metastable reaction. Graphite plus austenite form during the stable reaction. When eutectic solidification is complete, no liquid metal remains, and any further reaction takes place in the solid state.

## Slide 13
Although not shown in figure, in the temperature interval between the eutectic and eutectoid transformations, marked by points 3 and 4, the high-carbon austenite rejects carbon, which diffuses to the graphite flakes. This allows the austenite to acquire the composition needed for the eutectoid transformation, which, under equilibrium conditions, takes place between points 4 and 5. This transformation involves the decomposition of austenite into pearlite or pearlite plus ferrite, depending on such factors as the cooling rate and alloy content of the iron. In unalloyed gray irons, no significant changes in microstructure occur below the eutectoid transformation line.

## Slide 14
Carbon and silicon composition ranges of common cast irons and steel
Typical range for carbon and silicon contents in good-quality ductile iron.

## Slide 15
Typical flake graphite shapes. A, uniform distribution, random orientation; B, rosette groupings; C, kish graphite (superimposed flake sizes, random orientation); D, interdendritic segregation with random orientation; E, interdendritic segregation with preferred orientation
Characteristic cooling curves associated with different flake graphite shapes. TE, equilibrium eutectic temperature

## Slide 16
Type A graphite flakes are randomly distributed and oriented throughout the iron matrix. This type of graphite is found in irons that solidify with a minimum amount of undercooling, and type A is the structure desired if mechanical properties are to be optimized. Type B graphite is formed in irons of near-eutectic composition that solidify with a greater amount of undercooling than that associated with type A graphite and solidifying on a limited number of nuclei. Rosettes containing fine graphite, which are characteristic of type B, precipitate at the start of eutectic solidification. The heat of fusion associated with their formation increases the temperature of the surrounding liquid, thus decreasing the undercooling and resulting in the formation of type A graphite.

## Slide 17
Types D and E graphite form when the amount of undercooling is high but is not sufficient to cause carbide formation. Both types are found in interdendritic regions. Type D graphite is randomly distributed, while the type E flakes have a preferred orientation. Elements such as titanium and aluminum have been found to promote undercooled graphite structures. The iron matrix associated with undercooled graphite is usually ferrite because formation of the fine, highly branched flakes reduces carbon diffusion distances and results in a low-carbon matrix. Because ferrite has a lower tensile strength than pearlite, there is a reduction in the anticipated strength of the iron.

## Slide 18
General influence of carbon equivalent on the tensile strength of gray iron.
Effect of maximum graphite flake length on the tensile strength of gray iron

## Slide 19
Alloying elements
Alloying elements can be added in common cast iron to enhance some mechanical properties. They influence both the graphitization potential and the structure and properties of the matrix. The main elements are listed below in terms of their graphitization potential:
High positive graphitization potential (decreasing positive potential from left to right): C, Sn, P, Si, Al, Cu, Ni, Neutral, Fe
High negative graphitization potential (increasing negative potential from top to bottom left to right): Mn, Cr, Mo, V

## Slide 20
In general, alloying elements can be classified into three categories. Each is discussed below.
Silicon and aluminum increase the graphitization potential for both the eutectic and eutectoid transformations and increase the number of graphite particles. They form solid solutions in the matrix. Because they increase the ferrite/pearlite ratio, they lower strength and hardness
Nickel, copper, and tin increase the graphitization potential during the eutectic transformation, but decrease it during the eutectoid transformation, thus raising the pearlite/ferrite ratio. This second effect is due to the retardation of carbon diffusion. These elements form solid solution in the matrix. Because they increase the amount of pearlite, they raise strength and hardness.

## Slide 21
Chromium, molybdenum, tungsten, and vanadium decrease the graphitization potential at both stages. Thus, they increase the amount of carbides and pearlite. They concentrate in principal in the carbides, forming (FeX)nC-type carbides, but also alloy the α Fe solid solution. As long as carbide formation does not occur, these elements increase strength and hardness. Above a certain level, any of these elements will determine the solidification of a structure with both Gr and Fe3C (mottled structure), which will have lower strength but higher hardness.
In alloyed gray iron, the typical ranges for the elements discussed above are as follows: Cr: 0.2-0.6, Mo: 0,2-1,
V: 0.1-0.2, Ni: 0.6-1, Sn: 0.04-0.08

## Slide 23
Influence of inoculation on tensile strength as a function of carbon equivalent for 30 mm diam
bars.
Influence of graphite morphology on the stress-strain curve of several cast irons

## Slide 24: Spheroidization Techniques
Open crucible technique (Effeciency: 20%-30%)
Sandwich technique (Effeciency: 40%-45%)

## Slide 25
Plunging technique
(Effeciency: ~ 50%)
(Cored) Wire technique
(Effeciency: Higher than sandwich technique)

## Slide 26
Converter technique (Effeciency: ~ 50%)

## Slide 27
Küresel grafitin çekirdeklenmesi

## Slide 28
Influence of residual magnesium on graphite shape
Influence of residual magnesium (a) and nodularity (b) on some mechanical properties of ductile iron.

## Slide 29
The elements in the first group the spheroidizing elements can change graphite shape from flake through compacted to spheroidal. The most widely used element for the production of spheroidal graphite is magnesium. The amount of residual magnesium required to produce spheroidal graphite is generally 0.03 to 0.05 %. The precise level depends on the cooling rate. A higher cooling rate requires less magnesium. The amount of magnesium to be added in the iron is a function of the initial sulfur level.

## Slide 30
Östenit kılıfının oluşma hızı parçanın soğuma hızı, aşılama ve bazı kritik elementlerin varlığından etkileniyor. Soğuma hızının yüksek olması ve sıvının etkin bir şekilde aşılanmış olması, östenit kılıfının daha hızlı oluşmasını sağlıyor. Bu da küreselliğin korunabilmesini sağlıyor.
Alaşımda bulunan bazı elementler ise, bu kılıfın oluşma hızını düşürerek, grafit parçacıklarında biçimsel bozulmalara yol açıyor. Örnek vermek gerekirse Bi, Sb, Pb, Sn ve Al gibi elementlerin, grafitin biçimsel özelliklerini olumsuz bir şekilde etkilediğini ve küreselliği düşürdüklerini söyleyebiliriz.

## Slide 31: Video links
https://www.youtube.com/watch?v=8Z_z0jpUc34
https://www.youtube.com/watch?v=5ZtPvkSFLYA
https://www.youtube.com/watch?v=LZqemJmGyQg
https://www.youtube.com/watch?v=s2Ruajxm9Dw
https://www.youtube.com/watch?v=tNAQdKbLvWg