## Slide 1: Solidification of Single Phase Metals and Alloys (III)

## Slide 2: Structural effects resulting from solute redistribution in alloys

## Slide 3
In the case of both cells and cellular dendrites micro-segregation occurs. The intercellular regions are rich in solute for k0 < 1 and depleted of solute for k0 > 1

## Slide 4
Quantitative results on distribution of solute (coring) in columnar dendritic crystal

## Slide 5
Distribution of Cu in an Al-4.5% Cu alloy. Cu segregation: light contrast in microradiograph
Segregation in Al-Cu alloy
Both forms of segregation (micro and macro) can be eliminated by a homogenising heat treatment although of course macro-segregation effects involve long diffusion distances and thus long heat treatment times.

## Slide 6: Dendritic structures
The word dendrite comes from the Greek Word «dendron» that means tree.
Dendritic growth is strongly crystallographic. The primary arms and side branches have their arms parallel to specific crystallographic directions. For example, in FCC metals and alloys these are <001> directions. The growth forms are very varied. Normally each large branched dendrite grows from a single nucleus and has a single orientation. Small misorientations can be produced during growth by mechanical vibrations brought about by turbulence

## Slide 7
When dendritic growth occurs continuously over a large volume material the resultant structure is strongly anisotropic. This anisotropy can have quite deleterious effects on properties. For this reason steps are normally taken to promote profuse nucleation and provide maximum isotropy.
Structure | Metal | Dendrite normal direction
FCC | Lead | <001>
BCC | β-Brass | <001>
HCP | Zinc | <1010>
BCT | Tin | <110>

## Slide 8
Short dendrite (Cu-Zn)
Long dendrite (Cu-Sn)

## Slide 9: Solidification time and dendrite size
The rate at which growth of the solid occurs depends on the cooling rate, or the rate of heat extraction. A higher cooling rate produces rapid solidification, or short solidification times. The time ts required for a simple casting to solidify completely can be calculated using Chvorinov’s rule:

## Slide 10
where V is the volume of the casting and represents the amount of heat that must be removed before freezing occurs, A is the surface area of the casting in contact with the mold and represents the surface from which heat can be transferred away from the casting, n is a constant (usually about 2), and B is the mold constant. The mold constant depends on the properties and initial temperatures of both the metal and the mold. This rule basically accounts for the geometry of a casting and the heat transfer conditions. The rule states that, for the same conditions, a casting with a small volume and relatively large surface area will cool more rapidly.

## Slide 11
Effect on Structure and Properties The solidification time affects the size of the dendrites. Normally, dendrite size is characterized by measuring the distance between the secondary dendrite arms.The secondary dendrite arm spacing (SDAS) is reduced when the casting freezes more rapidly. The finer, more extensive dendritic network serves as a more efficient conductor of the latent heat to the undercooled liquid. The SDAS is related to the solidification time by
where m and k are constants depending on the composition of the metal.

## Slide 12
Dendrites in an aluminium alloy

## Slide 14
Interdendritic Shrinkage This consists of small shrinkage pores between dendrites. This defect, also called microshrinkage or shrinkage porosity, is difficult to prevent by the use of risers. Fast cooling rates may reduce problems with interdendritic shrinkage; the dendrites may be shorter, permitting liquid to flow through the dendritic network to the solidifying solid interface. In addition, any shrinkage that remains may be finer and more uniformly distributed.

## Slide 15
(a) Shrinkage can occur between the dendrite arms. (b) Small secondary
dendrite arm spacings result in smaller, more evenly distributed shrinkage porosity.
(c) Short primary arms can help avoid shrinkage. (d) Interdendritic shrinkage in an
aluminium alloy is shown (x 80).

## Slide 16: Grain structure formation in castings and macroscopic interface growth shapes
Orientation difference starts from nucleus growth. A nucleus rapidly grows until it is stopped by neighbours.

## Slide 19
Planar interface
Columnar coarse grains
Dendritic interface
Equiaxed fine grains

## Slide 20: Grain solidification and micro-segregation formation
The change in structure of a Cu-40% Ni alloy during equilibrium solidification. The nickel and copper atoms must diffuse during cooling in order to satisfy the phase diagram and produce a uniform equilibrium structure.

## Slide 21
The cooling curve for an isomorphous alloy during solidification. We assume
that cooling rates are low so that thermal equilibrium is maintained at each temperature. The changes in slope of the cooling curve indicate the liquidus and solidus temperatures, in this case, for a Cu-40% Ni alloy.

## Slide 22
The change in structure of a Cu-40% Ni alloy during non-equilibrium
solidification. Insufficient time for diffusion in the solid produces a segregated structure.

## Slide 23
Solidification, precipitation, and microstructure of a Pb-10 % Sn alloy. Some dispersion strengthening occurs as the β solid precipitates.

## Slide 24
Non-equilibrium solidification and microstructure of a Pb-15 % Sn alloy. A non-equilibrium eutectic micro-constituent can form if the solidification is too rapid.