## Slide 1: Aluminium Casting Alloys .

## Slide 2: Introduction
Aluminium casting alloys are the most versatile of all common foundry alloys and generally have the highest castability ratings. aluminium alloy castings are routinely produced by pressure-die, permanent-mold, green-and dry-sand, investment, and plaster casting. aluminium alloys are also readily cast with vacuum, low-pressure, centrifugal, and pattern-related processes such as lost foam. Casting alloys make up about 42% of annual aluminium production. Approximately 65% of this is used in die casting.
As casting materials, aluminium alloys have the following favorable characteristics:

## Slide 3
Good fluidity for filling thin sections
Low melting point relative to those required for many other metals
Rapid heat transfer from the molten aluminium to the mold, providing shorter casting cycles
Hydrogen is the only gas with appreciable solubility in aluminium and its alloys, and hydrogen solubility in aluminium can be readily controlled by processing methods
Many aluminium alloys are relatively free from hot-short cracking and tearing tendencies
Chemical stability
Good as-cast surface finish with lustrous surfaces and little or no blemishes

## Slide 4
The aluminium Association designation system attempts alloy family recognition by the following scheme:
1xx.x: Controlled unalloyed compositions
2xx.x: Aluminium alloys containing copper as the major alloying element
3xx.x: Aluminium-silicon alloys are also containing magnesium and/or copper
4xx.x: Binary aluminium-silicon alloys
5xx.x: Aluminium alloys containing magnesium as the major alloying element
6xx.x; Currently unused
7xx.x: Aluminium alloys containing zinc as the major alloying element, usually also containing additions of either copper, magnesium, chromium, manganese, or combinations of these elements
8xx.x Aluminium alloys containing tin as the major alloying element
9xx.x Currently unused

## Slide 5: Effects of Alloying Elements
Silicon. The outstanding effect of silicon in aluminium alloys is the improvement of casting characteristics. Additions of silicon to pure aluminium dramatically improve fluidity, hot tear resistance, and feeding characteristics. The most prominently used compositions in all casting processes are those of the aluminium-silicon family. Commercial alloys span the hypoeutectic and hypereutectic ranges up to about 25% Si. In general, an optimum range of silicon content can be assigned to casting processes. For slow cooling rate processes (such as plaster, investment, and sand), the range is 5 to 7%, for permanent mold 7 to 9%, and for die casting 8 to 12%. The bases for these recommendations are the relationship between cooling rate and fluidity and the effect of percentage of eutectic on feeding. Silicon additions are also accompanied by a reduction in specific gravity and coefficient of thermal expansion.

## Slide 6
Magnesium is the basis for strength and hardness development in heat-treated Al-Si alloys and is commonly used in more complex Al-Si alloys containing copper, nickel, and other elements for the same purpose. The hardening phase Mg2Si displays a useful solubility limit corresponding to approximately 0.70% Mg, beyond which either no further strengthening occurs or matrix softening takes place. Common premium-strength compositions in the Al-Si family employ magnesium in the range of 0.40 to 0.070%. Binary Al-Mg alloys are widely used in applications requiring a bright surface finish and corrosion resistance, as well as attractive combinations of strength and ductility. Common compositions range from 4 to 10% Mg, and compositions containing more than 7% Mg are heat treatable. Instability and room-temperature aging characteristics at higher magnesium concentrations encourage heat treatment.

## Slide 7
Copper. The first and most widely used aluminium alloys were those containing 4 to 10% Cu. Copper substantially improves strength and hardness in the as-cast and heat-treated conditions. Alloys containing 4 to 6% Cu respond most strongly to thermal treatment. Copper generally reduces resistance to general corrosion and in specific compositions and material conditions, stress corrosion susceptibility. Additions of copper also reduce hot tear resistance and decrease castability.
Zinc. No significant benefits are obtained by the addition of zinc to aluminium. Accompanied by the addition of copper and/or magnesium, however, zinc results in attractive heat treatable or naturally aging compositions. A number of such compositions are in common use. Zinc is also commonly found in secondary gravity and die casting compositions.

## Slide 8
Iron improves hot tear resistance and decreases the tendency for die sticking or soldering in die casting. Increases in iron content are however accompanied by substantially decreased ductility. Iron reacts to form a myriad of insoluble phases in aluminium alloy melts, the most common of which are FeAl3, FeMnAl6, and α-AlFeSi. These essentially insoluble phases are responsible for improvements in strength, especially at elevated temperature. As the fraction of insoluble phase increases with increased iron content, casting considerations such as flowability and feeding characteristics are adversely affected. Iron participates in the formation of sludging phases with manganese, chromium, and other elements.

## Slide 9
Titanium is extensively used to refine the grain structure of aluminium casting alloys, often in combination with smaller amounts of boron. Titanium in excess of the stoichiometry of TiB2 is necessary for effective grain refinement. Titanium is often employed at concentrations greater than those required for grain refinement to reduce cracking tendencies in hot short compositions.
Boron combines with other metals to form borides, such as Al2 and TiB2. Titanium boride forms stable nucleation sites for interaction with active grain-refining phases such as TiAl3 in molten aluminium.
Silver is used in only a limited range of aluminium-copper premium-strength alloys at concentrations of 0.5 to 1.0%. Silver contributes to precipitation hardening and stress corrosion resistance.

## Slide 10
Sodium modifies the aluminium-silicon eutectic. Its presence is embrittling in aluminium-magnesium alloys. Sodium interacts with phosphorus to reduce its effectiveness in modifying the eutectic and that of phosphorus in the refinement of the primary silicon phase.
Strontium is used to modify the aluminium-silicon eutectic. Effective modification can be achieved at very low addition levels, but a range of recovered strontium of 0.008 to 0.04% is commonly used. Higher addition levels are associated with casting porosity, especially in processes or in thick-section parts in which solidification occurs more slowly. Degassing efficiency may also be adversely affected at higher strontium levels.
Phosphorus. In AlP3 form, phosphorus nucleates and refines primary silicon-phase formation in hypereutectic Al-Si alloys. At parts per million concentrations, phosphorus coarsens the eutectic structure in hypoeutectic Al-Si alloys. Phosphorus diminishes the effectiveness of the common eutectic modifiers sodium and strontium.

## Slide 11
Chromium additions are commonly made in low concentrations to room temperature aging and thermally unstable compositions in which germination and grain growth are known to occur. Chromium typically forms the compound CrAl7, which displays extremely limited solid-state solubility and is therefore useful in suppressing grain growth tendencies. Sludge that contains iron, manganese, and chromium is sometimes encountered in die casting compositions, but it is rarely encountered in gravity casting alloys. Chromium improves corrosion resistance in certain alloys and increases quench sensitivity at higher concentrations.
Manganese is normally considered an impurity in casting compositions and is controlled to low levels in most gravity cast compositions. Manganese is an important alloying element in wrought compositions, through which secondary foundry compositions may contain higher manganese levels. In the absence of work hardening, manganese offers no significant benefits in cast aluminium alloys. Some evidence exists, however, that a high volume fraction of MnAl6 in alloys containing more than 0.5% Mn may beneficially influence internal casting soundness.

## Slide 12
Tin is effective in improving antifriction characteristics, and is therefore useful in bearing applications. Casting alloys may contain up to 25% Sn. Additions can also be made to improve machinability. Tin may influence precipitation hardening response in some alloy systems.
Nickel is usually employed with copper to enhance elevated-temperature properties. It also reduces the coefficient of thermal expansion.
Lead is commonly used in aluminium casting alloys at greater than 0.1% for improved machinability.

## Slide 14: Grain Structure
A fine, equiaxed grain structure is normally desired in aluminium castings. The type and size of grains formed are determined by alloy composition, solidification rate, and the addition of master alloys (grain refiners) containing intermetallic phase particles, which provide sites for heterogeneous grain nucleation.
Grain Refinement Effects. A finer grain size promotes improved casting soundness by minimizing shrinkage, hot cracking, and hydrogen porosity. The advantages of effective grain refinement are:

## Slide 15
Improved feeding characteristics
Increased tear resistance
Improved mechanical properties
Increased pressure tightness
Improved response to thermal treatment
Improved appearance following chemical, electrochemical, and mechanical finishing
As-cast Al-7Si ingots showing the effects of grain refinement. (a) No grain refiner. (b) Grain refined.

## Slide 16
Grain Refinement. All aluminium alloys can be made to solidify with a fully equiaxed, fine grain structure through the use of suitable grain-refining additions. The most widely used grain refiners are master alloys of titanium, or of titanium and boron, in aluminium. aluminium-titanium refiners generally contain from 3 to 10% Ti. The same range of titanium concentrations is used in Al-Ti-B refiners with boron contents from 0.2 to 1% and titanium-to-boron ratios ranging from about 5 to 50. Although grain refiners of these types can be considered conventional hardeners or master alloys, they differ from master alloys added to the melt for alloying purposes alone. To be effective, grain refiners must introduce controlled, predictable, and operative quantities of aluminides (and borides) in the correct form, size, and distribution for grain nucleation.

## Slide 17: Modification and Refinement of Aluminium-Silicon Alloys
The addition of certain elements, such as calcium, sodium, strontium, and antimony, to hypoeutectic aluminium-silicon alloys results in a finer lamellar or fibrous eutectic network. It is also understood that increased solidification rates are useful in providing similar structures. There is, however, no agreement on the mechanisms involved. The most popular explanations suggest that modifying additions suppress the growth of silicon crystals within the eutectic, providing a finer distribution of lamellae relative to the growth of the eutectic. Various degrees of eutectic modification are shown in figure below.

## Slide 18
Varying degrees of aluminium-silicon eutectic modification ranging from unmodified (A) to well modified (F).

## Slide 19
Very low sodium concentrations (~0.001%) are required for effective modification. More typically, additions are made to obtain a sodium content in the melt of 0.005 to 0.015%. Remodification is performed as required to maintain the desired modification level.
A much wider range of strontium concentrations is in use. In general, addition rates far exceed those required for effective sodium modification. A range of 0.015 to 0.050% is standard industry practice. Normally, good modification is achievable in the range of 0.008 to 0.015% Sr. Remodification through strontium additions may be required, although retreatment is less frequent than for sodium.

## Slide 20
Mechanical properties of as-cast A356 alloy tensile specimens as a function of modification and grain size.

## Slide 21
Effect of phosphorus refinement on the microstructure of Al-22Si-1Ni-1Cu alloy. (a) Unrefined. (b) Phosphorus-refined.
(c) Refined and fluxed.
The elimination of large, coarse primary silicon crystals that are harmful in the casting and machining of hypereutectic silicon alloy compositions is a function of primary silicon refinement. Phosphorus added to molten alloys containing more than the eutectic concentration of silicon, made in the form of metallic phosphorus or phosphorus-containing compounds such as phosphor-copper and phosphorus pentachloride, has a marked effect on the distribution and form of the primary silicon phase. Investigations have shown that retained trace concentrations as low as 0.0015 through 0.03% P are effective in achieving the refined structure.

## Slide 22: Hydrogen in aluminium
Liquid aluminium actively dissolves hydrogen, which forms as a result of chemical reaction with water vapor:
2Al + 3H2O  Al2O3 + 6H
Sources of hydrogen in molten aluminium:
Atmosphere humidity;
Wet metallic charge;
Wet furnace lining (crucible, transfer ladles);
Wet foundry instruments;
Wet fluxes and other consumables;
Furnace fuel combustion products containing hydrogen.

## Slide 23
Solubility of hydrogen in aluminium at 1 atm hydrogen pressure.
Aluminium alloys release excessive amount of hydrogen during solidification. This results in porosity defects distributed throughout the solid metal. Size of the hydrogen pores and their quantity is determined by the initial content of hydrogen, the alloy composition and the solidification conditions.

## Slide 24: Reduced Pressure Test (RPT)

## Slide 26
Degassing by fluxes
Fluxes composed of chlorine and fluorine containing salts are used for degassing molten aluminium alloys. Degassing fluxes are commonly shaped in form of tablets. Degassing operation starts when a flux tablet is plunged by a clean preheated perforated bell to the furnace bottom. The flux components react with aluminium forming gaseous compounds (aluminium chloride, aluminium fluoride). The gas is bubbling and rising through the melt. Partial pressure of hydrogen in the formed bubbles is very low therefore it diffuses from the molten aluminium into the bubbles. The bubbles escape from the melt and the gas is then removed by the exhausting system. The process continues until bubbling ceases.

## Slide 28
Rotary degasser
In the rotary degassing method an inert or chemically inactive gas (Argon, Nitrogen) is purged through a rotating shaft and rotor. Energy of the rotating shaft causes formation of a large number of fine bubbles providing very high surface area-to volume ratio. Large surface area promotes fast and effective diffusion of hydrogen into the gas bubbles resulting in equalizing activity of hydrogen in liquid and gaseous phases. Rotary degasser allows achieve more complete hydrogen removal as compared to the flux degassing. Additionally rotary degasser does not use harmful chlorine and fluorine containing salts.
Rotary degasser may also combine the functions of degassing and flux introduction. In this case the inert gas serves as carrier for granulated flux. The method is called flux injection.

## Slide 31: Uses of Fluxes in Molten Aluminium Processing
Molten salt fluxes play an important role in the processing of molten aluminium. Most salt fluxes are based on either the KCl-NaCl or the KCI-MgCl2 binary systems. Additives include other chlorides, fluorides, nitrates, carbonates or sulphates. They are used either in a passive role to cover the metal from oxidation or sometimes in an active role to remove inclusions, alkali metals and magnesium. Salt fluxes can also be used to improve metal recovery from drosses as well as during melting of recycled scrap.

## Slide 32
Solid fluxes are mainly blends of chloride and fluoride salts with additives to instill special properties. Most fluxes are based on a mixture of KCl and NaCl, which forms a low-temperature (665°C) eutectic. Another common ingredient in fluxes is NaF, which forms a ternary eutectic with KCl and NaCl with a melting point of 607°C. A common cover flux contains about 47.5% NaCl, 47.5% KCl, and 5% fluoride salt. A low melting point is important since it will improve the fluidity of the flux.

## Slide 33
Other cover fluxes are based on MgCl2-KCl, which forms a low melting eutectic at 424°C, or carnalite (MgCl2×KCl), which melts at 485°C. These cover fluxes have high fluidity and can form a thin layer on the melt surface. However, MgCl2 is fairly expensive, so it is primarily used in sodium-free fluxes for alloys containing more than 2 wt.% magnesium. They may also be used where it is important to remove calcium in alloys of fairly high magnesium content.

## Slide 34
Alkali-fluoride salts have a slight (although very small) solubility of oxides, which facilitates penetration into oxide films that contain metallic aluminum in dross and build-up. This leads to improved wettability, favoring separation of oxide inclusions from the melt and metallic aluminum from the dross. Unfortunately, the high melting points of alkali-fluoride salts thicken the liquid flux, limiting their use. Also, the disposal of used fluoride-containing salts are subject to stricter environmental regulations than pure chloride salts. Fluxes may contain fluoride salts, such as cryolite (Na3AlF6), calcium fluoride (CaF2), and sodium silicofluoride (Na2SiF6), in amounts up to 20 percent.

## Slide 35: Video links
https://www.youtube.com/watch?v=sPyL9iszB4M
https://www.youtube.com/watch?v=enSCH7LF9Rc